05.10.2011

DISCUSSION PAPER – DRAFT

Subject: Classes in the Future hEN 10080

The draft of PrEN 10080 “Steel for reinforcement of concrete – Weldable reinforcing steel – General “ is at the final evaluation within ECISS/TC 104 "Concrete reinforcing and pre-stressing steels" (end of commenting period: 29th September).

This prEN has been elaborated on the basis of Mandate M/115 (date: May, 1997).

In the point 1 of the Annex 3 of this Mandate, regarding levels or classes, it is reported that:

1. 	Levels and classes for product performances

For the time being, the differences specified in Article 3 (2) of the CPD, do not seem to give rise to the need of a classification system for products.

Further needs may be identified on the basis of differences specified in Article 3 (2) of the CPD, which are justified in conformity with Community law (IDs Clause 1.2.1). Where for such needs it is recognised that a classification of product performance is the means of expressing the range of requirement levels of the works, the Commission will give the appropriate guidance or will request CEN/CENELEC to make the appropriate proposal through a modification to this mandate.

In the Foreword of the current draft of the prEN 10080 is reported that

“This document does not define levels or classes. They should be defined in accordance with this document by specified values for Rm, Re, Agt, Rm/Re, Re,act./Re,nom. (if applicable), fatigue strength (if required), cyclic load strength (if required), strength at elevated temperature (if required), bendability, weldability, bond strength, strength of welded or clamped joints (for welded fabric or lattice girders) and tolerances on dimensions.”.

Therefore the technical body of CEN has decided to not apply or define classes for this product.

This is not in accordance with the National Technical Rules for R.C. constructions of some Member States (in particular Italy and Germany), which requires (as regulated parameter/class) the declaration of the class of the steel according to EC2 (UNI EN 1992-1-1, Appendix C). In fact, in Italy be used only (ribbed or intended) reinforcement steel of class B 450 C or, for non seismic applications, B 450 A whereas in Germany may be used only B500 steel.

These Technical rules (e.g. the Italian one) and EC2 give the criteria to define these classes.

On the basis of these technical rules, the personnel responsible for the safe execution of works in these M.S. shall verify first of all, immediately and before the use, the class of the reinforcing steel to be used in the r.c. structures; the declared parameters considered in the current version of pr10080 are not enough to determine, immediately, these classes.

Therefore, in the future EN10080, should be considered the declaration of the class of steel (according to EC2) and also the declaration of the ratios between characteristic and nominal (according to the class) values of the tensile and tensile yield strengths should be declared, in order to verify the complying with the national rules.