COMMISSION IMPLEMENTING DECISION

of XXX

on the classification without further testing of wood-based panels in accordance with EN 13986 and of solid wood panelling and cladding in accordance with EN 14915 as regards their fire protection ability

THE EUROPEAN COMMISSION,

Having regard to the Treaty on the Functioning of the European Union,

Having regard to Council Directive 89/106/EEC of 21 December 1988, on the approximation of laws, regulations and administrative provisions of the Member States relating to construction products, and in particular Article 20(2) thereof,

Whereas:

- Council Directive 89/106/EEC envisages that in order to take account of different levels of protection for the construction works at national, regional or local levels, it may be necessary to establish in the interpretative documents classes corresponding to the performance of products in respect of each essential requirement. Those documents have been published as the “Communication of the Commission with regard to the interpretative documents of Directive 89/106/EEC.”

- With respect to the essential requirement of safety in the event of fire, interpretative document No 2 lists a number of interrelated measures which together define the fire safety strategy to be variously developed in the Member States.

- Paragraph 4.3.1.3 of interpretative document No 2 identifies one of these measures prevailing in Member States that relates to the resistance to fire performance of construction products and/or parts of construction works.

- By way of a harmonised solution, a system of classes was adopted in Commission Decision 2000/367/EC of 3 May 2000 implementing Council Directive 89/106/EEC as regard the classification of the resistance to fire performance of construction products, construction works and parts thereof .

- To express the fire protection ability of wood-based panels, solid wood panelling and cladding, all used for wall and ceiling covering, it is necessary to use the classification established in Decision 2000/367/EC.

- The fire protection ability of wood-based panels, solid wood panelling and cladding, all used for wall and ceiling covering, within the classification provided for in Decision 2000/367/EC, is well established and sufficiently well known to fire regulators in Member States that they do not require testing for this particular performance characteristic.

- The measures provided for in this Decision are in accordance with the opinion of the Standing Committee on Construction,

HAS ADOPTED THIS DECISION:

Article 1

The construction products and/or materials which satisfy all the requirements of the performance characteristic “fire protection ability” without need for further testing are set out in the Annex.

Article 2

The specific classes to be applied to different construction products and/or materials, within the resistance to fire classification adopted in Decision 2000/367/EC, are set out in the Annex to this Decision. Products shall be considered in relation to their end-use application, where relevant.

Article 3

This Decision shall enter into force on the first day following that of its publication in the Official Journal of the European Union.

Done at Brussels,

For the Commission

On behalf of the President 
	Antonio Tajani
	Vice President

ANNEX

The table set out in this Annex, lists construction products and/or materials which satisfy all of the requirements for the fire protection ability performance without need for testing.

TABLE: CLASSES OF FIRE PROTECTION ABILITY PERFORMANCE

FOR WOOD-BASED PANELS AND FOR SOLID WOOD PANELLING AND CLADDING USED FOR WALL AND CEILING COVERING

| Product 1) | EN product standard | Product detail 2) | Minimum mean density (kg/m3) | Minimum thickness (mm) | K Class |
| --- | --- | --- | --- | --- | --- |
| Hardboard | EN 13986 | With and without tongue and groove 4) | 800 | 9 | K2 10 3) |
| OSB | EN 13986 | With and without tongue and groove 5) | 600 | 10 | K2 10 3) |
| Particleboard | EN 13986 | With tongue and groove 6) | 600 | 10 | K2 10 2) |
| Particleboard | EN 13986 | With and without tongue and groove 5) | 600 | 12 | K2 10 3) |
| Plywood | EN 13986 | With and without tongue and groove 5) | 450 | 12 | K2 10 3) |
| Solid wood panels | EN 13986 | With and without tongue and groove 5) | 450 | 12 | K2 10 3) |
| Particleboard | EN 13986 | With tongue and groove 7) | 600 | 25 | K2 30 |
| OSB | EN 13986 | With tongue and groove 7) | 600 | 30 | K2 30 |
| Plywood | EN 13986 | With tongue and groove 7) | 450 | 26 | K2 30 |
| Solid wood panels | EN 13986 | With tongue and groove 7) | 450 | 26 | K2 30 |
| Solid wood panels | EN 13986 | With tongue and groove 8) | 450 | 53 | K2 60 |
| Solid wood panelling and cladding | EN 14915 | With tongue and groove 9) | 450 | 15 | K2 10 3) |
| Solid wood panelling and cladding | EN 14915 | With tongue and groove 9) | 450 | 27 | K2 30 |
| Solid wood panelling and cladding | EN 14915 | With tongue and groove 10) | 450 | 2 x 2711) | K2 60 |

- Mounted directly on any substrate without an air gap.

- Joints with square edges or tongue and groove profile and with the same thickness as the wood product and without gaps.

- K1 10 for substrates ≥ 300 kg/m3

- Brad length minimum 40 mm and spacing maximum 100 mm

- Screw length minimum 30 mm and spacing maximum 200 mm

- Screw length minimum 30 mm and spacing maximum 150 mm

- Screw length minimum 50 mm and spacing maximum 200 mm

- Screw length minimum 75 mm and spacing maximum 200 mm

- Nail length minimum 60 mm and spacing maximum 600 mm

- Nail length minimum 50 mm (in each layer) and spacing maximum 600 mm

11)	The two layers are mounted with the longitudinal direction of the layers perpendicular to each other.

OJ L 40, 11.2.1989, p. 12.

OJ C 62, 28.2.1994, p. 1

OJ L 133, 6.6.2000, p. 26 as amended by Decision 2003/629/EC (OJ L 218, 30.8.2003, p. 51).